## Slide 1: eP5XLE Detector Design Change
Bottom Detector (BBD) Charging Solution

## Slide 2: Summary
BBD New design vs Old design
SiO2 700nm
SiO2 200nm
Uniform Ti/Au coating
active area
Smooth sidewall polish
New BBD
Old BBD
Rough sidewall polish
Non-uniform Ti/Au coating
active area
SiO2 grinded
 | New | Old
Image shift | Good | OK, large variation
Fine Focus drift | Good | Good
Stig drift | Good | Bad (drifting)
* New design uses SE signal, and old design uses BSE signal due to driver shortage. The difference between 2 types of signals have no impact on the test results.